## Slide 1
Polymer Basic Training
Seminar 2
CATS Calculation & Design Tools
Presenter
Application Development Automotive
Date

## Slide 2
Content
What can we do for customer?
Concept design
Design optimization
Moldflow calculation
FEM calculation
High efficient cooperation?

## Slide 3
Modelling (CAD)
  NX-IDEAS
  NX9.0
  CATIA V4 & V5
Finite Element Analysis (FEA)
  IDEAS
  NX NASTRAN
  ANSYS
  ABAQUS
Moldflow
  Autodesk Moldflow Insight
Mesh Tool
  Hypermesh
Topology & Shape Optimization
  TOSCA
Material Simulation
  DIGIMAT
Fatigue
  FEMFAT
Crash
  LS-DYNA
CAE Software Portfolios
*Softwares marked by blue can only be supported by ADC Switzerland currently.

## Slide 4
Simulation VS molding trial results
Moldflow Support: Warpage Prediction
Calculated gap between two parts
Gap between two injected parts

## Slide 5
Moldflow Support: Gating System Optimization
3D blow molding
Overmouldling
EMS solution:
Material: Tube Grilon EBGM-20H
Bracket Grilon BG-15 FC

## Slide 6
Moldflow Support: Gating System Optimization
The tube is remelted during overmouldling.
Original gate
Optimized gate
By optimizing gating system and process, problems have been solved!

## Slide 7
Moldflow Support: Gating System Optimization
Melt velocity decrease around 30%
Original gate
Injection pressure decrease to 20%
By using more gate

## Slide 8
Moldflow Support: Warpage Optimization
Large Shrinkage
large Shrinkage
Fiber orientation

## Slide 9
Moldflow Support: Warpage Optimization
Small Shrinkage
Small Shrinkage
Fiber orientation
Warpage reduced to 1/3 compared to original gate position

## Slide 10
Equivalent stress
Grivory GVX-65H
FEM Analysis: Gear Mesh Stress Calculation

## Slide 11
1. principal stress
2. principal fibre orientation
FEA
rheology
Principal stress can be viewed in Moldflow through second development using VB
FEM Analysis: Gear Mesh Stress Calculation

## Slide 12
Water Tap Breakage Analysis
Stress plot
Runner System

## Slide 13
Water Tap Breakage Analysis
Principal stress
Weldline
Principal stress is perpendicular to the weldline, breakage will happen under high torque.

## Slide 14
Weldline were shifted to low stress areas and the part can pass the torque test!
Water Tap Breakage Analysis
Original design
Recommended design
Create 0.25mm deeper slots as flow brake.
High stress

## Slide 15
MFA+FEM : Using Metal Insert if Necessary
Breakage occurred at the weldline!

## Slide 16
MFA+FEM : Using Metal Insert if Necessary
84MPa
152MPa
95MPa
The redesigned part fulfills test requirements.

## Slide 17
Normal mode results at peak of A,B,C,D
Mode1 : 117Hz
Mode3 : 233Hz
Mode5 : 350Hz
Vibration Analysis of Air Duct

## Slide 18
What Do We Need?
CAD File (*.stp, UG file, Checklist, Objective)
How the part works? (principle, loading)
Test conditions and test results
CAE report done by customer for reference

## Slide 19
Application:
Clutch Master Cylinder (CMC) Housing
New Design or Metal Replacement:
Metal Replacement
Cost Estimation Calculation
Before you submit the request, please think below questions ahead:
Cost estimation calculation needs to be done firstly

## Slide 20
Current Solution: Al Die-Cast
Weight of Metal Part: CNY 17.80
Cost of Metal Part: 223 g
Potential: 20,000 pcs/a
Customer Part Nr.: T22 041 021
Material for Calculation: Grilon TSG-35/4 W2
          Black 9839
Cost Estimation Calculation Sample

## Slide 21
Note: the recommendations and data given are based on our experience to date, however, no liability can be assumed in connection with their usage and processing.
 | Favorable | Unfavorable
Injection Molding Cost per Part [CNY] | 11.79 | 14.29
Die Cast Cost per Part [CNY] | 17.80 | 17.80
Cost Savings [%] | 34 | 20
Weight Savings [%] | 43 | 38
Cost Estimation Calculation Sample

## Slide 22
Chart: Estimated Production Costs Metal Replacement
| favourable | unfavourable
Insert Parts | 2.3 | 2.5
Re-machining Costs | 0.10833 | 0.15556
Personnel Costs | 0.62087 | 0.77634
Tool Costs | 1.1 | 1.2
Machine Costs | 1.4805 | 1.8909
Material Costs | 6.1755 | 7.7636
The cost difference is: 17%
14.29 CNY
Cost Estimation Calculation Sample

## Slide 23
Product
Definition
Product Development
Product Conception
Production
100%
0%
Cost
Influence Potential
Cost
Generation Potential
Virtual Prototyping (CAE) = High Leverage
CAE as a problem solver
= Lower leverage
The Earlier, The Better

## Slide 24
FEM Analysis: Piston Breakage Analysis
Directly replace aluminum with plastic, stress level is higher than allowable strength for selected material.
Add ribs
Original design
200MPa!
Optimized design

## Slide 25
FEM Analysis: Piston Breakage Analysis
Without consideration of fiber orientation
78MPa
Considering fiber orientation
90MPa
Fatigue strength at 1M cycles is 80MPa.

## Slide 26
FEM Analysis: Piston Breakage Analysis
Difference between S-N curve test and load condition in reality, mean stress influence.
Test condition
Real load condition
The optimized part can pass the life test!
Why?

## Slide 27
Project Workflow : Steering Lock Housing
Metal replacement project
The part must pass the 300N.m torque test.
Critical areas
Zinc die casting weight: 450g
Using GV grade material plus metal insert: 150g

## Slide 28
Project Workflow : Steering Lock Housing
0 MPa
210 MPa
FEM analysis to check the feasibility of replacement

## Slide 29
Project Workflow : Steering Lock Housing
Good agreement between simulation and prototype test results.

## Slide 30
Project Workflow : Steering Lock Housing

## Slide 31
Project Workflow : Steering Lock Housing
Metal insert solution to compensate the strength of the part

## Slide 32: Disclaimer
The information contained in this publication is based on our present know-ledge and experience. The given figures and data are guidance values and do not represent binding material specifications. No warranties of any kind, either express or implied, including warranties of merchantability or fitness for a particular purpose, are given regarding products, design, data and information. The customer is not released from his obligation to investigate the products fitness and the suitability for the intended application, compliance with legal requirements and intellectual property rights. We reserve the right to change the information at any time and without prior notice. The information in this publication is not to be considered a contractual obligation and any liability whatsoever is expressly declined. For further questions about our products please contact our experts.